## Slide 1
Physical Electronics Ⅱ
Semiconductor Electronics Ⅱ
TCAD simulation : MOSFET

## Slide 2: Content
Introduction
Long channel MOSFET
Body effect
Non-ideal effects
Short channel effects
Summary

## Slide 3: Content
Introduction
Long channel MOSFET
Body effect
Non-ideal effects
Short channel effects
Summary

## Slide 4: Reference
1 μm 공정은 1980년대 쓰이던 공정 기술
이시기에 상용화된 제품 중 Intel386TM SX MICROPROCESSOR data sheet 참고
동작 전압 5.0 V로 설정하여 시뮬레이션 진행

## Slide 5: Device structure
Parameters | Values
Lg | 1 μm
Lsd | 0.5 μm
Tbody | 1.2 μm
Tsd | 0.3 μm
Tox | 0.02 μm
Nbody | Boron 1017 cm-3
Nsd | Arsenic 1020 cm-3
S/D Gaussian factor | 0.35
Source
Nsd
Gate oxide (SiO2)
Gate (TiN)
Lg
Tsd
Tbody
Lsd
Tox
Drain
Nsd
Body
Nbody

## Slide 6: Content
Introduction
Long channel MOSFET
Body effect
Non-ideal effects
Short channel effects
Summary

## Slide 7: Operation region
Accumulation
Depletion
Threshold
Strong inversion
Source
Nsd
Gate oxide (SiO2)
Gate (TiN)
Drain
Nsd
Body
Nbody
VGS -1.0 V ~ 3.0 V
VDS 5.0 V
cut-line
M
O
S
M
O
S
M
O
S
Flat band
M
O
S
M
O
S

## Slide 8: Operation region (Accumulation)
Accumulation
M
O
S

## Slide 9: Operation region (Flat band)
Flat band
M
O
S

## Slide 10: Operation region (Depletion)
Depletion
M
O
S

## Slide 11: Operation region (Threshold)
Threshold
M
O
S

## Slide 12: Operation region (Strong inversion)
Strong inversion
M
O
S

## Slide 13: Content
Introduction
Long channel MOSFET
Body effect
Non-ideal effects
Short channel effects
Summary

## Slide 14: Body effect
Source
Nsd
Gate oxide (SiO2)
Gate (TiN)
Drain
Nsd
Body
Nbody
VGS -1.0 V ~ 3.0 V
VDS 5.0 V
VBS 0.0, -1.0, -2.0 V
Body effect
VBS [V] | Vth [V]
0.0 | 1.37
-1.0 | 1.81
-2.0 | 2.12
Inspect tool 활용하여 Vth 추출
Vth 증가
Lg = 1.00 μm

## Slide 15: Body effect
Source
Nsd
Gate oxide (SiO2)
Gate (TiN)
Drain
Nsd
Body
Nbody
VGS 0.0 V
VDS 0.0 V
VBS 0.0, -1.0, -2.0 V
cut-line
M
O
S
M
O
S
M
O
S

## Slide 16: Content
Introduction
Long channel MOSFET
Body effect
Non-ideal effects
Short channel effects
Summary

## Slide 17: Channel length modulation
Lg = 1.00 μm
Lg = 0.48 μm
channel length
modulation

## Slide 18: Velocity saturation
Lg = 1.00 μm
Lg = 0.48 μm
Long channel
Short channel
Physics의 mobility ( HighFieldSaturation )
적용시 Velocity saturation 구현 가능

## Slide 19: Content
Introduction
Long channel MOSFET
Body effect
Non-ideal effects
Short channel effects
Summary

## Slide 20: ID-VG
Punch-through
GIDL
Vth roll-off

## Slide 21: Vth roll-off
Lg = 1.00 μm
Lg = 0.57 μm

## Slide 22: Vth roll-off
Lg [μm] | Vth [V]
1.00 | 1.37
0.57 | 1.04
0.48 | 0.58
0.45 | 0.13
Vth roll-off
Vth는 ID = 10-7 A/μm x (W/L) [A/μm] 에서 추출
(강의 자료 W10-2 p.366 참고)

## Slide 23: DIBL
Lg = 1.00 μm
High VDS = 5.0 V, Low VDS = 0.1 V
DIBL
Lg [μm] | DIBL [mV/V]
1.00 | 4.49
0.57 | 53.27
* Vth (inspect tool) 추출 하여
DIBL 계산
source
channel
drain
source
channel
drain
Lg = 0.57 μm

## Slide 24: Punch through
Lg = 1.0 μm
Lg = 0.45 μm
VGS = -1.0 V, VDS = 5.0 V
punch through

## Slide 25: Punch through
Lg = 0.45 μm
VGS = -1.0 V, VDS = 5.0 V
cut-line
cut-line
source
channel
drain
source
bulk
drain
barrier
drift

## Slide 26: GIDL
Lg = 1.00 μm
VGS = -1.0 V, VDS = 5.0 V
Over lap
BTBT
source
channel
drain
drain
SiO2
gate
Physics의 recombination (Band2Band (E1))
적용시 BTBT구현 가능
* band-to-band-tunneling (BTBT)
cut-line
cut-line
BTBT

## Slide 27: GIDL
Lg = 1.00 μm
VGS = -1.0 V, VDS = 5.0 V
High E-field
cut-line

## Slide 28: Content
Introduction
Long channel MOSFET
Body effect
Non-ideal effects
Short channel effects
Summary

## Slide 29: Summary
ID-VD
ID-VG
Channel length
decrease
Lg [μm] | Vth [V] | SS [mV/dec] | DIBL [mV/V]
1.00 | 1.37 | 111.63 | 4.49
0.57 | 1.04 | 108.99 | 53.27
0.48 | 0.58 | 131.83 | 124.29
0.45 | 0.13 | 337.94 | 202.86